Aggregation of magnetic nanoparticles functionalized with trans-resveratrol in aqueous solution

Thi-Nga Nguyen1,2,3, Quang-Hung Tran4, Clarence Charnay5, Xavier Dumail5, Corinne Reibel5, Guillaume Cazals6, Gilles Valette6, Christian Jay-Allemand1, Ferial Terki2, Luc P. R. Bidel7

1UMR IATE, University of Montpellier, Institut Agro, INRAE, F-34060 Montpellier, France.

2PhyMedExp UMR CNRS 9214 – Inserm U1046, 34295 Montpellier Cedex 05, France.

3Institute of Natural Products Chemistry, Vietnam Academy of Science and Technology, 18 Hoang Quoc Viet, 100000 Hanoi, Vietnam.

4eV-Technologies, 2 Esplanade Anton Philips, Bâtiment 5, 14460 Colombelles, France.

5Institut Charles Gerhardt UMR 5253 CNRS-UM, Université de Montpellier, F-34095 Montpellier, France.

6IBMM UMR5247, CNRS, ENSCM, Université de Montpellier, Place Eugène Bataillon, 34095 Montpellier Cedex 5, France

7UMR AGAP, University of Montpellier, CIRAD, INRAE, Institut Agro, Montpellier, France.

Corresponding: luc.bidel@inrae.fr

## Supporting information

S1. Silanization of trans-resveratrol

Figure S1: Transmittance spectra as a function of the wavenumber of the reaction process at 7 hours and 3 days recorded by attenuated total reflection of the infrared spectrometer.

Figure S2: Structure of silanized trans-resveratrol and their numbering of the carbon skeletons: 1, 2, 3 corresponding to the silane derivatives binds covalently to the three, two, and one hydrogen bonding sites of the trans-resveratrol molecule, respectively. Arrows show the key C-H correlations on the HMBC of compounds 2 and 3.

S2. Dynamic light scattering measurement

Figure S3: Size distribution of nanoparticles in absolute ethanol and in TRIS buffer at pH 10.0.

S3. Zeta potential measurement

Figure S4: Distribution of zeta potential of nanoparticles at different pH.

S4. Extinction Cross-section

Table S1: The parameters of the Rayleigh-Gans-Debye model As(λ)=W.λ-ndeduced from the linear fitting of the logarithm of extinction as a function of the logarithm of the wavelength.

| pH | Compound | W | n |
| --- | --- | --- | --- |
| 3.0 | CS1 | 8.68 | 1.14 |
|  | CS2 | 0.86 | 0.77 |
|  | CS3 | 10.65 | 1.17 |
| 5.0 | CS1 | 9.65 | 1.15 |
|  | CS2 | 23.70 | 1.26 |
|  | CS3 | 60.79 | 1.42 |
| 7.0 | CS1 | 298.61 | 1.60 |
|  | CS2 | 378.79 | 1.60 |
|  | CS3 | 2618.78 | 1.81 |
| 10.0 | CS1 | 59006.52 | 2.39 |
|  | CS2 | 19760.59 | 2.19 |
|  | CS3 | 233292.08 | 2.57 |

S5. Appendix NMR spectra of compound 1, 2, and 3

Figure S5: NMR spectra of compound 1, 2, and 3

S6. Mass spectroscopy of compound 1, 2, and 3.

MALDI-TOF Compound 1

MALDI-TOF Compound 2

MALDI-TOF Compound 3