High-Performance Sustainable Tissue Paper from Agricultural Residue: A Case Study on Fique Fibers from Colombia

Rajnish Kumar, Franklin Zambrano, Ilona Peszlen, Richard Venditti, Joel Pawlak, Hasan Jameel, Ronalds Gonzalez*

Tissue Pack Innovation Lab, Department of Forest Biomaterials, North Carolina State University, Raleigh, North Carolina, USA, 27695-8005

(*) Corresponding author: R. Gonzalez (rwgonzal@ncsu.edu)

Figure A 1. Zero span tensile strength (expressed as breaking length) of fique residue and NBSK pup measured at different pulp freeness. Error bars represent one standard deviation.

Zero Span Tensile Strength

Figure A 2. Tensile stiffness of fique residue bleached pulp and NBSK pulp at different pulp freeness. Tensile stiffness was measured from the stress-strain curve generated during the tensile testing by the Instron. Error bars represent one standard deviation.

Tensile stiffness of individual pulps

Figure A 3. Surface smoothness/roughness (TS750) of individual pulps plotted against the tensile index of tissue handsheets. A lower value represents smoother surface. Error bars represent one standard deviation

Surface Smoothness/Roughness (TS750) of Individual Pulps

Figure A 4. Surface smoothness/roughness (TS750) of pulp blends plotted against the tensile index of tissue handsheets. A lower value represents smoother surface. Error bars represent one standard deviation.

Surface Smoothness/Roughness (TS750) of pulp blends