Substances	Quantity/Concentration	Supplier	Use
PBS + penicillin and streptomycin	1% penicillin and streptomycin	PBS (Biowest, France) / Penicillin and streptomycin (Lonza, Belgium)	Adipose tissue washing before digestion
Collagenase I	0.02%	(Sigma-Aldrich, USA)	Tissue digestion

Table S1. Substances used in hADMSCs isolation and culture

Protocol details
Digestion with Collagenase I DMEM solution: shaking for 2h at 37ºC / Cell suspension filtration: with a 40µm cell strainer (Corning, USA) / Cells centrifugation: 1700 rpm for 10 minutes / Expansion medium composition: high-glucose DMEM media (Lonza, Belgium) supplemented with 10% FBS (Gibco, ThermoFisher scientific, USA) and 1% P/S (Lonza, Belgium)

Table S2. Protocol details in hADMSCs isolation and culture

Substances	Quantity/Concentration	Supplier	Use
Ethanol	70%	-	Samples sterilization (overnigth)
PBS	-	-	Samples washing
Neutral red solution	0,1%	Scharlab, Spain	Citotoxity test

Table S3. Substances used in Citoxity tests

Protocol details
Wells seeded with a density of 4·104 cells/ml/cm2 without contact with samples were used as controls (blanks). / MTS solution was prepared at 42mg/ml in PBS and 1ml of PMS (Phenazine methosulfate; Sigma Aldrich, Germany) at 0.92mg/ml was mixed with 20ml of MTS solution prior to use.

Table S4. Protocol details in Citotoxity tests

Substances	Quantity/Concentration	Supplier	Use
Human pooled whole blood anti-coagulated with Li-heparin from 3 donors	-	3 donors	TBH obteining (by mixing the blood with Drabkin’s reagent)
Poly-L-Lysine in sterile distilled water	1% (10 mg/mL)	Sigma-Aldrich, Germany	Positive Control (PC)
Polyethylene glycol in water	40%	Sigma Aldrich, Germany	Negative Control (NC)

Table S5. Substances used in Haemolysis index determination

Protocol details
Samples incubation: 3h at 37°C and inverted every 15min / Tubes centrifugation: 800rpm for 15min / The quantitative determination for Hb was made by creating a standard curve by two fold serial dilution of Hb (from 1.20 mg/ml to 0.01 mg/mL).

Table S6. Protocol details in Haemolysis index determination

Substances	Quantity/Concentration	Supplier	Use
Dexamethasone	0.1µM	Sigma-Aldrich, USA	differentiation medium supplement
Ascorbic acid	50µM	Sigma-Aldrich, USA	differentiation medium supplement
β-glycerol phosphate	10mM	Sigma-Aldrich, USA	differentiation medium supplement

Table S7. Substances used in Osteogenetic differenciation

Substances	Quantity/Concentration	Supplier	Use
PBS	-	-	Differentiated osteogenic cells washing before and after fixation
Formaldehyde	4%	Merck, Germany	Fixation (15 minutes)
BCIP/NBT solution	-	SIGMA FAST™ BCIP/NBT, Sigma-Aldrich, USA	Cell staining (for 45 minutes at room temperature)

Table S8. Substances used in Alkaline phosphatase staining

Substances	Quantity/Concentration	Supplier	Use
PBS	-	-	Differentiated osteogenic cells washing before fixation
Paraformaldehyde	10%	-	Cells fixation (for 45 minutes at 4°C)
Distilled water	-	-	cells washing after fixation
Alizarin red solution	2%	Merck, Germany	Cell staining (for 5 minutes at room temperature)

Table S9. Substances used in Alizarin red staining

Protocol details
The quality of the RNA was assessed through absorbance measurements made using a NanoDrop ND-1000 UV–Vis Spectrophotometer (NanoDropTechnologies, Wilmington, DE). All the samples used in the PCR procedures showed a 260/280 nm absorbance ratio between 1.8 and 2.2. A ratio of approximately 2 is accepted as pure for RNA. / Reverse transcription was carried out with the iScript cDNA Synthesis Kit (Bio-Rad, Hercules, CA) / The cDNA samples, stored at -20°C until use, were cooled at 4°C.

Table S10. Protocol details in RNA extraction

Protocol details
The primers for the CASPASE 3 and β-ACTIN genes examined were designed by Beacon Designer software (Premier Biosoft International, CA). The other genes were designed for Sigma Aldrich KiCqStart TM SYBR® Green Primers (Sigma Aldrich, USA). / SYBR Green PCR Supermix (2X) (Bio-Rad), which detects amplification using Sybr Green as a double-stranded DNA specific fluorescent dye, was used as the mastermix. / Assays in duplicate and a blank was included in every assay were performed. / The reaction mixture for amplification comprised 2µL of cDNA, 0.4µL of each primer (forward and reverse primers; final concentration 0.1µM), 10µL of Sybr Green mix and sterile water in a final volume of 20µL. / For the Sparc gene, the reaction mixture for amplification comprised 2µL of cDNA, 1.8µL of each primer (forward and reverse primers; final concentration 450nM), 10µL of Sybr Green mix and sterile water in a final volume of 20µL. / The RT-PCR protocol, in the case of CASPASE-3 and β-ACTIN, included an initial step of 95°C (5 min), followed by 45 cycles of 15 sec at 94°C for DNA denaturation, 30 sec for primer annealing at 60°C and 1 minute at 55,7°C for primer extension. Table S13 provides more information about the RT-PCR parameters.

Table S11. Protocol details in RT-PCR

Gene	Annealing temperature (Cº)	Melting temperature (Cº)	Sequence (5’-3’)		Amplicon Size (bp)
ALPL	59 °C	85.5°C	F-AGT
			R-CGTCCCG
- ACTIN	57.0 °C	88.5°C	F- ACTACCTCATGAAGATCCTC
			R- CGGATGTCCACGTCACACTTC
BGLAP	63.3 °C	83.5°C	F-TTCTTTCCTCTTCCCCTTG	97
			R-CCTCTTCTGGAGTTTATTTGG
CASPASE-3	57 °C	83°C	F-CTGGACTGTGGCATTGAGAC	159
			R- ACAAAGCGACTGGATGAACC
COL1	63.3 °C	89.5°C	F-GCTATGATGAGAAATCAACCG	199
			R-TCATCTCCATTCTTTCCAGG
IBSP	63.3 °C	77°C	F-GGAGACTTCAAATGAAGGAG	80
			R-CAGAAAGTGTGGTATTCTCAG
SPARC	60 °C	80°C	F-AGTATGTGTAACAGGAGGAC	143
			R-AATGTTGCTAGTGTGATTGG

Table S12. Genes, annealing and melting temperatures, primer sequences and amplicon sizes of human genes tested by RT-PCR.